SECTION 098310 - ACOUSTICAL PANELS

GENERAL

SUMMARY

This Section includes the following:

Acoustical melamine foam panels.

SUBMITTALS

Product Data:  Submit manufacturer’s technical data for each type of acoustical panel required.

Shop Drawings:  Submit shop drawings showing how panels are to be laid out on walls and ceilings.  Width of panels and location of vertical seams.

QUALITY ASSURANCE

Single-Source Responsibility:  Provide acoustical panel units and installation components by a single manufacturer.

Fire Performance Characteristics:  Identify acoustical wall components with appropriate markings of applicable testing and inspecting organization.

Surface Burning Characteristics:  Class A, tested per ASTM E 84.

Flame Spread:  25 or less.

Smoke Developed:  200 or less.

Coordination of Work:  Coordinate acoustical panel work with installers of related work including, but not limited to building insulation, gypsum board, light fixtures, mechanical systems, electrical systems, and sprinklers.

DELIVERY, STORAGE, AND HANDLING

Deliver acoustical panels to project site in original, unopened packages and store them in a fully enclosed space where they will be protected against damage from moisture, direct sunlight, surface contamination, and other causes.

Before installing acoustical panels, permit them to reach room temperature and stabilized moisture content.

Handle acoustical panels carefully to avoid chipping edges or damaged units in any way.

PRODUCTS

MANUFACTURERS

Acoustical Panels:

Acoustical Melamine Foam Panels by Acoustical Surfaces, Inc. (Basis of Design)

123 Columbia Court North, Suite 201, Chaska, MN 55318.

952-448-5300, Fax: 952-448-2613.

Toll Free: 1-800-448-3134.

Or equal.

ACOUSTICAL PANELS

Product: Acoustical Melamine Foam Panels.

Material: Open Cell Melamine Acoustical Foam.

Pattern: Flat.

Features: Designed for sound absorption in a wide range of frequencies. Increased surface absorption area.

Thickness: 1 or 2 inches.

Sizes: 2 by 2 feet or 2 by 4 feet.

Edge Detail: Square. Optional half-beveled edge.

Density: 0.7lbs/cu. ft.

Colors:

Standard Colors: Natural White or Light Grey.

Latex or HPC Paint: Black, Light Grey, or Almond.

Painted: Black, Brown, Beige, Light Gray or custom colors available.

Flammability: ASTM E84, Class A.

Flame Spread: 6.

Smoke Developed: 15.

Noise Reduction Coefficient:

1 inch: .060.

2 inch: 1.00.

Installation:

Acoustical Adhesive.

Also available as hanging acoustical baffles.

Applications: Industrial, Commercial, Audio, OEM Residential Markets, Ceilings, Walls, Partitions, Sound/Recording Studios, Radio Stations, Board Rooms, Swimming Pools, Churches, Schools, Gun Ranges, Enclosures.

EXECUTION

PREPARATION

Measure each area and establish layout of acoustical units to balance border widths at opposite edges of each area.  Coordinate metal panel layout with mechanical and electrical fixtures.

INSTALLATION

Install panels per the manufacturer’s written instructions.

CLEANING

Clean exposed panel surfaces.  Comply with manufacturer's written instructions for cleaning, and minor finish damage repairs.  Remove and replace panel components that cannot be successfully cleaned and repaired to permanently eliminate evidence of damage, including deformed panels.

END OF SECTION 098310